No. 2177-03 CycLoops FrameGuard Bike Rack

Bicycle Rack shall be CycLoops® FrameGuard™ model No. 2177-03 in the material and color finish selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company.  Phone 800/547-1940.  www.timberform.com

1.  Materials

Bicycle Rack shall be mild steel or stainless steel tube and bar.  Standard surface mount bases shall be manufactured from 1/4 inch thick mild steel plate, permanently welded and include two 5/8” dia. holes each for anchor bolts furnished by installing contractor.  Protective side cushions shall be black Santoprene®

2.  Construction

Curved Bicycle Rack shall be derived from a constant 1’ 4-5/8” radius bend through 306 degrees.   Bending that distorts the tubing is not allowed.  Bicycle Rack shall be deburred and ground smooth after fabrication.  Santoprene® shall be permanently affixed using aluminum mono-bolts.

3.  Finish

(-C) Steel shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.

-or-

(-G)  Mild steel bicycle rack shall be hot-dipped galvanized per ASTM 123 after complete fabrication.

-or-

(-S)  Stainless steel bicycle rack shall have No. 4 polish finish.