No. 2174 Wall CycLoops Bicycle Rack

Bicycle Rack shall be TimberForm® Wall CycLoops™ model No. 2174, to accommodate one bicycle, in color or finish selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

Bicycle Rack shall be single loop of 1 inch i.d. schedule 40 mild steel seamless pipe with a minimum wall thickness of .133 inch.  Easily vandalized thin wall tubing is not allowed.  Loop shall include a pre-drilled flange permanently welded to ends which will accommodate two half inch diameter wall anchor bolts (contractor supplied).

2.  Construction

Bicycle Rack shall be a single unit.  Bicycle Rack shall be deburred and ground smooth after fabrication.

3.  Finishes

Steel and cast iron parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.

-or-

Mild steel (-G) bicycle rack shall be hot-dipped galvanized per ASTM 123 after complete fabrication.

-or-

Stainless steel (-S) bicycle rack shall have No. 4 polish finish.